## Slide 1: NIR emission from hBN

## Slide 2
Microscope
Physical pinhole
1:1 relay lens
XY stage
Telescopic Z stage
50/50 Splitter
Multimode Fibre
Camera
Timecard
0
1
OPO SHG fs pulsed laser (80MHz)
Imaging Spectrometer
LP Filter
LP Filters
Filters to clean pump
APDs
Confocal Set-up
Sample on XYZ scanning stage
to Labview Interface

## Slide 3: hBN on Quartz: Area scanned
M = 10X
M = 111X

## Slide 4
532nm pump (0.2mW before objective)
Nikon 60X 0.95NA
75 micron pinhole
VIS collection (650nm - ~850nm)
NIR collection (>900nm)
Anti-bunched emission observed in VIS but not NIR
(same excitation conditions as above for coincidences, integration time 10 minutes, coincidence window 0.5ns)
10um
10um

## Slide 5
680nm pump (2mW before objective)
Olympus 100X (111X with Nikon tube lens) 0.85NA
200 micron pinhole
VIS collection (650nm - ~850nm)
NIR collection (>900nm)
25um
25um

## Slide 6
Anti-bunching in NIR emission:
Id320 detector efficiency 20% @ 1550nm, dead time 2us
680nm pump, 2mW before objective; collection>750nm
Integration time 4 hrs, coincidence window 0.5ns
NIR collection (>900nm)
25um
(no background subtraction)

## Slide 7: Further Work
Background should probably be retaken, for full 4hr length (above was coincidences over 10 minutes multiplied by 24)
What should be the analytic expression for the fit function?
Most efficient pump wavelength was found to be 635nm, re-take at this pump?
Basic background subtraction & fit